Cetol Filter 7

A translucent satin gloss woodfinish for exterior

use, based on special alkyd resins with built-in UV filters and transparent iron oxides.

General

Main properties	Excellent resistance to UV-rays, which guarantees a permanent

flexibility.

Its high absorption of UV-rays ensures optimum wood protection.

Weather-resistant.

Its high transparency ensures optimum visibility of the wood grain.

Microporous.

Water-repellent.

No dirt retention.

Simple maintenance.

Very easy application.

Use	Protection and decoration of hard- and softwood exterior joinery.

Application data

Application temperature	5 – 35°C

At temperatures below 10°C, the drying process will be delayed.

R.H. max. 90 %

Application method	By brush.

Dilution	None. Ready for use after stirring thoroughly.

Cleaning of equipment	Clean brushes and equipment in white spirit.

Practical coverage	Approx. 16 m²/l per coat

The coverage depends very much on the wood species to be

treated, the method of application and the conditions of

application.

Advised layer thickness	Dry: Approx. 15 µm per coat

Wet: Approx. 40 µm

A Cetol Filter 7 system should have a minimum dry film thickness

of 40 µm.

Drying at 20°C/65% RH	Dust free: after approx. 4 hours

Recoatable: after approx. 16 hours

Properties

Package viscosity	0,12 Pa.s/23°C

Density	Approx. 0,90 kg/dm³

Solids content	By weight: approx. 45%

By volume: approx. 38%

Gloss level	Satin gloss finish (25-30 G.U./60° ASTM D 523)

Flow	Good flow, ensuring maximum and uniform film thickness.

Outdoor durability	Very good (3-4 years if used in a Cetol Filter 7 system).

Durability depends to a large extend on location, elevation and by

the quality of wood, design, construction, glazing, condition of

interior paintwork, method of application, etc.

Shelf life	At least 12 months, if stored in unopened packing.

Additional information

Packaging	1 l – 2,5 l – 5 l

Colour range	Available in 8 translucent colours:

006 Light oak – 009 Dark oak – 010 Walnut – 020 Ebony

045 Mahogany – 048 Rosewood – 077 Deal – 085 Teak

All colours can be intermixed in any proportion. The final colour of

the Cetol Filter 7 finish also depends on the wood species to

which it is applied.

Systems	Timber quality:

Wooden exterior window frames, windows and doors should meet

the quality standards for joinery (STS 52 – 1973 by N.I.H.).

New woodwork:	Apply one priming coat of Cetol Novatech in selected colour.

Where necessary, stop with tinted putty. Sand slightly and remove

dust.

Apply 2 finishing coats of Cetol Filter 7. For best results, it is

necessary to keep the interval between application of these coats

as short as possible. This period should not exceed 5 months.

Do not sand in between the various coats of Cetol Filter 7.

Maintenance:	Depending on the condition of the finish, clean down and sand

down thoroughly. Repair any defects and apply one further coat of

Cetol Filter 7 overall.

Remarks	Covering of horizontal surfaces:

During construction, it is recommended to cover horizontal

surfaces with plastic or aluminium foil to prevent their

discolouration by mortar and cement.

Merbau:	Merbau contains dark-coloured extractives that easily dissolve in

water and leach out (bleeding). To prevent this process, Merbau

elements should not be installed untreated in houses under

construction, but previously be treated in the joiners shop with a

minimum of two coats of Cetol Filter 7. On site, complete the

system by applying one or two coats of Cetol Filter 7.

Treatment of rebates, elements 	Always apply two coats of material to rebates, glazing beads (on

to be concealed by brickwork:	all faces), backs of cladding, etc.

Treat surfaces to be concealed by brickwork previously with two

coats of Cetol Novatech.

Application on top of other products:	Cetol Filter 7 can also be applied over intact translucent stain,

Cetol THB and Cetol HLS coatings. Strip off defective coatings

completely and proceed as specified for new work.

Health and safety information

Flash point (DIN 53213)	+ 40°C.

Transport code (ADR/VLG)	3 - 31 c.

Please revert to the Material Safety Data Sheet for additional information.